## Slide 1
Bulk Topological Superconductor

## Slide 2: Possible Topological Superconductors
Z
Time-Reversal Invariant (TRI)
Time-Reversal Broken (TRB)
1D
2D
3D
Z2
Z2
Z2
Z
-
Schnyder-Ryu-Furusaki-Ludwig (2008)
Kitaev (2009)
“Periodic Table” of topological invariant
Chiral p-wave
SC in TI surface
Surface State of TIs
Bogoliubov qp
EF
TI
SC
SC
f = 0
f = p
Fu & Kane (2008)
EF
2D
Majorana
Edge State
Sr2RuO4
(D)
(DIII)

## Slide 3: Possible Topological Superconductors
Z
Time-Reversal Invariant (TRI)
Time-Reversal Broken (TRB)
1D
2D
3D
Z2
Z2
Z2
Z
-
Schnyder-Ryu-Furusaki-Ludwig (2008)
Kitaev (2009)
“Periodic Table” of topological invariant
Kitaev model
1D Nanowire of InSb or InAs
Majorana
End-State
Alicea, RPP (2012)
Oreg et al., PRL (2010)
Lutchyn et al., PRL (2010)
Chiral p-wave
SC in TI surface
Mourik et al., Science (2012)
Das et al., Nature Phys. (2012)
InSb/
NbTiN
InAs/Al
(D)
(DIII)

## Slide 4: Possible Topological Superconductors
Z
Time-Reversal Invariant (TRI)
Time-Reversal Broken (TRB)
1D
2D
3D
Z2
Z2
Z2
Z
-
Schnyder-Ryu-Furusaki-Ludwig (2008)
Kitaev (2009)
“Periodic Table” of topological invariant
Kitaev model
Superfluid 3He-B phase
The surface state may host
Helical Majorana Fermions
that are itinerant and massless
E
ky
EF
New 3D topological state of matter
Chiral p-wave
SC in TI surface
(D)
(DIII)

## Slide 5: SC in CuxBi2Se3
Hor et al., PRL (2010)
Conventional SC State in the bulk
 Proximity SC
E
k
EF
Topological SC
State in the bulk
Fu & Berg, PRL (2010)
E
k
EF
 Helical Majorana fermions
Four-component Hamiltonian of Bi2Se3
with the basis
(  P1z+,  P1z+,  P2z-,  P2z- )
Majorana zero mode in vortices
Hosur et al., PRL (2011)

## Slide 6: SC in CuxBi2Se3
Hor et al., PRL (2010)
Conventional SC State in the bulk
 Proximity SC
E
k
EF
Topological SC
State in the bulk
Fu & Berg, PRL (2010)
E
k
EF
 Helical Majorana fermions
Zero Resistivity
Specific Heat Jump
SC V.F.
 70%
Problem:
Sample is difficult to prepare, shielding fraction is low.
Majorana zero mode in vortices
Hosur et al., PRL (2011)

## Slide 7: “Soft” Point Contact
SEM image of an actual sample
(Ag particle size ~50 nm)
Sasaki, Ando et al., PRL (2011)
Ag particles on the surface
Sn
CuxBi2Se3
T-dep.
B-dep.
Notes: 7

## Slide 8
Effects of Heating and/or Critical Currents?
Example of a spurious ZBCP
G(V)/Gn
V (mV)
0
0 T
0.5 T
0.75 T
1 T
Sheet et al., PRB (2004)
Dip position moves with H
Peak height is insensitive to H
T = 0.35 K
H dependence is completely
different!
H-dep.
Reflectionless tunneling would
be governed by Lf ~ 1 mm and
suppressed with ~1 mT.
Andreev bound state due to an unconventional SC state
Notes: 8

## Slide 9: Possible SC States in CuxBi2Se3
Four-component Hamiltonian of Bi2Se3 (  P1z+,  P1z+,  P2z-,  P2z- )
Sasaki, Ando et al., PRL (2011)
All odd-parity states are topologically non-trivial and host helical Majorana fermions on the surface
Fu & Berg, PRL (2010)

## Slide 10: Unconventional SC States in CuxBi2Se3
D2 : Odd parity, full gap
D4 (D3) : Odd parity, point node
Helical Majorana A
Hsieh & Fu, PRL(2012)
Helical Majorana B
Helical Majorana C
Yamakage et al., PRB (2012)
dI/dV for A
dI/dV for B
dI/dV
Sasaki, Ando et al., PRL (2011)
ZBCP due to helical Majorana fermions?

## Slide 11: Controversy in CuxBi2Se3
Conventional s-wave ?
STM
Levy et al.,
PRL (2013)
If the bulk is BCS s-wave
Parity mixing of pair potential is anomalously enhanced by surface Dirac fermions
EF
Mizushima, Yamakage,
Sato & Tanaka, PRB (2014)
Opening of an additional surface gap which is larger than the bulk gap
?

## Slide 12: Controversy in CuxBi2Se3
n  1017 cm-3
1019 cm-3
1020 cm-3
Lahoud et al.,
PRB (2013)
n = 2  1020 cm-3
n = 4  1017 cm-3
Levy et al.,
PRL (2013)
Quasi-2D TSC?
Mizushima et al., arXiv:1311.2768

## Slide 13
Superconducting Doped TCI

## Slide 14: Topological Crystalline Insulator SnTe
SnTe
Hsieh et al., Nature Commun. (2012)
PbTe
SnTe
: contribution from Te p-orbital
SnTe
PbTe
Band inversion + Mirror symmetry
 Nontrivial Mirror Chern number
ky
p
0
L1
L2
L3
L4
p
kx
+
-
-
+
Z2 invariant n = 0
Tanaka, Sato, Ando et al.,
Nature Physics (2012)

## Slide 15: In-doped SnTe Superconductor
n = 2 – 8  1020 cm-3
Sn1-xInxTe
Erickson et al., PRB (2009)
Ferro-
electric
NaCl Structure
Te2-
Sn2+/In3+
Sato, Ando et al., PRL (2013)
Topological SS is present in Sn1-xInxTe.
Rhombohedral
Cubic
Novak, Ando et al.,
PRB (2013)

## Slide 16: In-doped SnTe
Sn1-xInxTe
(x = 0.045)
B- dep.
Tc = 1.2 K
Faceted (001) surface
T- dep.
0.24 meV  2D
Peak suppression
corresponds to Hc2
Normalized ZBCP height is > 2 !!
Surface Andreev Bound State due to Unconventional SC
Point-Contact Spectroscopy
Sasaki, Fu, Ando et al., PRL (2012)

## Slide 17: SnTe vs. PbTe
SnTe
PbTe
Tanaka, Ando et al., Nature Phys. (2012)
T- dep.
T- dep.
Sn1-xInxTe
Pb1-xTlxTe
Conventional
Similar FS structures, but the band parities are different.
Unconventional

## Slide 18: Possible SC States in Sn1-xInxTe
kp Hamiltonian of SnTe around each L point
sz = 1  p orbitals of Sn and Te with opposite parity
( k3: along GL, k1: along LK )
Possible Pairing Symmetry
(representations of D3d group)
Parity
A1g
A1u
A2u
Eu
even
odd
odd
odd
Topologically non-trivial
Topological SC?
kp Hamiltonian of Bi2Se3 around G point
sz = 1  Se pz orbitals on the top and bottom layer
Sasaki, Fu, Ando et al.,
PRL (2012)

## Slide 19: Possible SC States in Sn1-xInxTe
Possible Pairing Symmetry
(representations of D3d group)
Parity
A1g
A1u
A2u
Eu
even
odd
odd
odd
Topologically non-trivial
Rhombohedral
Cubic
Novak, Ando et al.,
PRB (2013)
Topological SC?
Sasaki, Fu, Ando et al.,
PRL (2012)

## Slide 20: Majorana Zero Mode in Vortices?
CuxBi2Se3
Majorana zero mode in vortices
Hosur et al., PRL (2011)
Sn1-xInxTe
Multiple Majorana zero modes can coexist due to additional symmetry to protect them from hybridization
If the bulk SC is conventional:

## Slide 21
Natural Heterostructure

## Slide 22: Natural Heterostructure PSBS
[(PbSe)5]n[(Bi2Se3)3]m
n = 1
m = 1
m = 2
m = 
(Bi2Se3)
(Bi2Se3)
“Quintuple Layer”
Nakayama, Sato, Ando et al., PRL (2012)

## Slide 23: Natural Heterostructure PSBS
Y. Zhang, Q.K. Xue et al., Nat. Phys. (2010)
m = 1
m = 2
m = 
Surface states are encapsulated by the insulating PbSe layer
Quasi-2D system with topological “bulk” state !!
“Surface states” in every (Bi2Se3)m units?
Ultra-thin Bi2Se3 Films
Nakayama, Sato, Ando et al., PRL (2012)

## Slide 24: Cu-intercalation to PSBS m = 2
Sasaki, Segawa, Ando, PRB (2014)

## Slide 25: Nearly 100% Volume Fraction
Specific-heat behavior is very different from BCS, suggesting a gap with line nodes
Sasaki, Segawa, Ando
PRB (2014)

## Slide 26: Reproducibility
Cel(T) is reproducible in two high-volume-fraction samples.
Sasaki, Segawa, Ando
PRB (2014)

## Slide 27: Magnetic-Field Dependence of Cel
At low T, , pointing to the existence of line nodes.
Sasaki, Segawa, Ando
PRB (2014)

## Slide 28: Implications of Cu-PSBS
Nodal Gap  Unconventional SC
None of the previously known superconducting TI presented clear bulk signature of unconventional SC
Sign Changing Gap + Strong Spin-Orbit Coupling  Spin-split surface Andreev bound state (i.e. Helical Majorana fermions)
Quasi 2D-Fermi surface  Majoranas are on the side
surface or terrace edge
d-wave gap

## Slide 29
SrPtAs

## Slide 30
SrPtAs

## Slide 31
Stronger relaxation in the SC state
Appearance of spontaneous magnetic field
TRS breaking
T-dependence of penetration depth
Full gap
d+id (chiral d-wave) pairing ?

## Slide 32
Thank you!